VOLUMETRIC – COMPLEXOMETRIC METHOD FOR THE DETERMINATION OF SULFATE IN CHROMIUM PLATING SOLUTIONS

Alex Sirota & Vera Persits

Chemical Laboratory, Materials and Processes Engineering, Engines Division, IAI, Lod, Israel

E-mail: alsirota@iai.co.il

The quality of chromium deposition in chromium plating process is depended on catalyst concentration in the plating solution. Most industrial chromium plating solutions use sulfate, sometimes with other ions, as a catalyst. Controlling the amount of catalyst in the chromium plating solution is critical – if there is out of the limits, no chromium will be deposited.

This paper suggests a number of improvements to the classic sulfate analysis, which enable the fast and accurate sulfate determination using simple procedure and equipment available in every industrial laboratory.

References:

- Kenneth E. Langford , Janet E. Parker “Analysis of electroplating and related solutions”, Fourth Edition, Robert Draper Ltd., 1971.

- Frank J. Welcher, ”The analytical uses of Ethylene diamine tetraacetic acid.”, 
Toronto-London-New York, 1961.

- Lurie Y.Y, Ribnikova A.I., Chemical analysis of Wastewater, Moscow, 1974.

- White W.W., Henry M.C., ” The determination of sulfate in chromium plating baths by EDTA titration.,” Plating, May 1972, p.429-430.