ION-SELECTIVE ELECTRODE BASED 
ON IONIC LIQUIDS WHICH ARE SOLID AT ROOM TEMPERATURE

Natalia  Shvedene,  Denis Chernyshov, Oksana  Avramenko, Larisa Tomilova, 
Igor Pletnev

Department of Chemistry, M.V. Lomonosov Moscow State University, 
Russian Federation,

shvedene@analyt.chem.msu.ru

During recent years Room-Temperature Ionic Liquids (RTIL) were increasingly widely applied in electrochemical sensors for the detection of ions in aqueous solution [1,2], in particular, ion-selective electrodes (ISE) with plasticized polymer membranes [3]. In ISE membrane, RTIL can play a role of plasticizer, of ion-exchanger, or the both. Liquid- and solid-contact versions of ISE were produced [4]. In all the cases, however, using RTIL in electrochemical sensor requires a presence of embedding polymeric media, in order to create a stable ion-sensitive layer. We introduced and investigated a rather different approach to the design of ion-sensing layer by using ionic liquids which melt above room temperature (low-melting ionic solids, LMIS). While heated and being liquid, they may be conveniently used to cover various surfaces; after cooling, they form a solid coating on the surface. This procedure takes a few minutes and requires nothing except a simple laboratory hot-plate. Typically, LMIS demonstrate good adhesion towards various substrates (metals, plastics, carbon materials, etc.).  In particular, we fabricated electrochemical sensors by immobilization of LMIS on the conductive surface of commercially available screen-printed electrodes.

The ion-sensing layers form such materials are not only plasticizer- free, but also polymer-free. Finally, it is highly important that LMISs may be easily doped (in liquid state) by various selective ionophores.  To our mind, usage of LMTSs is interesting for producing screen-printed electrodes (SPE) with differently modified surfaces.

Ionic liquids 1,3-dihexadecylimidazolium nitrate (DHDImNO3, tm=68.5 oС) 1 and 1-dodecyl-3-methylimidazolium hexafluorophosphate (DDMImPF6, Тпл=70 oС) 2 with  PctCoI 3 was used to fabricate SPE ISE  as sensors for inorganic anions - NO3 - and I -, respectively.

This work was supported by the INTAS (grant 05-1000008-8020).

References

[1]  D. Wei, A. Ivaska. Anal. Chim. Acta. 607 (2008) 126.

[2] N.V. Shvedene, D.V. Chernyshov, I.V. Pletnev. J. Russ. Chem. Soc. 52 (2008) 80.

[3] N.V. Shvedene, D.V. Chernyshov, M.G. Khrenova, A.A. Formanovsky, V.E. Baulin, I.V. Pletnev. Electroanalysis. 18 (2006) 1416.

[4] D.V. Chernyshov, M.G. Khrenova, I.V. Pletnev, N.V. Shvedene. Mend. Commun. 18 (2008) 88.