METAL-ENHANCED BIOLUMINESCENCE: AN APPROACH FOR MONITORING BIOLOGICAL LUMINESCENT PROCESSES

Evgeni Eltzov,1 Daria Prilutsky,2,3,4 Ariel Kushmaro,4,5 Robert S. Marks,4,5,6,7 and Chris D. Geddes7

1Unit of Environmental Engineering, Faculty of Engineering Science, Ben-Gurion University of the Negev, Beer-Sheva, Israel

2Department of Virology, Faculty of Health Science, Ben-Gurion University of the Negev, Beer-Sheva, Israel 85104

3Department of Information Systems Engineering, Faculty of Engineering Science, Ben-Gurion University of the Negev, Beer-Sheva, Israel

4National Institute of Biotechnology in the Negev, Ben-Gurion University of the Negev, Beer-Sheva, Israel5Department of Biotechnology Engineering, Faculty of Engineering Science, Ben-Gurion University of the Negev, Beer-Sheva, Israel

6The Ilse Katz Center for Meso and Nanoscale Science and Technology, Ben-Gurion University of the Negev, Beer-Sheva, Israel

7The Institute of Fluorescence, Medical Biotechnology Center, University of Maryland BiotechnologyInstitute, 701 East Pratt St, Baltimore, Maryland 21202, USA

In this research, the observation of metal (plasmon)-enhanced bioluminescence is reported. Bacteria, which are capable of generating specific bioluminescence signatures upon metabolic changes (general toxicity), have been studied from both glass and silvered glass microwell bottoms, where the silvered microwells have been modified with surface deposited silver island films (SiFs). The presence of the SiFs plasmon amplifies the near-field bioluminescence signatures, < 50 nm from the surface, enabling amplified detection of the reporter bioluminescence indicating sample toxicity. Using our approach a greater than fivefold enhancement in far-field bioluminescence occurs with much greater enhancements in the near-field predicted. Whole cell optic biosensors have been already proposed for use in many environmental applications.1,2 Thus, increasing the light intensity will invariably increase the sensitivity and eventually the attractiveness of these constructs in the future.

1      R. S. Marks, D. C. Cullen, I. Karube, C. R. Lowe, and H. H. Weetall, [Handbook of Biosensors and Biochips] [Wiley, New York] [2007].

2     T. Fine, P. Leskinen, T. Isobe, H. Shiraishi, M. Morita, R. S. Marks, and M. Virta, [Biosens. Bioelectron] [21] [2263-2269] [2006]