NEW MIXED-MODE METHACRYLATE-BASED POLYMERIC MONOLITHS PREPARED VIA COMPLEXATION WITH CYCLODEXTRINS EMPLOYED AS STATIONARY PHASES FOR CAPILLARY ELECTROCHROMATOGRAPHY AND µ-LIQUID CHROMATOGRAPHY

Fuad Al-Rimawi *, Ute Pyell **

* Faculty of Science and Technology, Al-Quds University, P.O. Box 20002, East Jerusalem,

fuad_rimawi@bpc.ps

** Department of Chemistry, University of Marburg, Hans-Meerwein-Strasse, D-35032 Marburg, Germany,

pyell@chemie.uni-marburg.de

Employing solubilization by complexation with cyclodextrins, new mixed-mode monolithic stationary phases for capillary electrochromatography (CEC) and µ-liquid chromatography were synthesized. Free radical copolymerization was performed in aqueous solution with a cyclodextrin-solubilized hydrophobic monomer, a water-soluble crosslinker (piperazinediacrylamide), and a charged monomer (vinylsulfonic acid). Different hydrophobic methacrylate monomers (isobornyl-, adamantyl-, cyclohexyl-, and phenyl methacrylate) were investigated. Chromatographic properties of the synthesized monoliths were studied with aqueous and non-aqueous mobile phases with hydrophobic and with polar analytes. Due to the amphiphilic nature of the polymers synthesized, the elution orders obtained correspond to the reversed-phase mode and to the normal-phase mode dependent on the polarity of the mobile phase. However, observations made with polar solutes and polar mobile phase can only be explained by a mixed-mode retention mechanism. Run-to-run, day-to-day, and capillary-to-capillary reproducibility of electroosmotic mobility and retention factors were determined. Comparison of retention data with those of a commercial octadecyl silica gel HPLC column reveals that the methylene selectivity of the monolithic capillaries prepared in this study is very similar to that of routinely used octadecyl silica gels.