PRECONCENTRATION OF URANIUM(VI) WITH

SORBTION – PHOTOMETRIC METHODS

Abel Maherramov, Sevindj Hachiyeva, Fidan Bahmanova,

Sahil Hamidov, Famil Chiragov

Baku State University, Chemistry department, 
Z. Khalilov, 23 street, Az 1148 Baku, Azerbaijan

Fidancem-82@rambler.ru

Keywords: uranium (VI), preconcentration, polymer sorbent, sorbtion, determination

In the presented work has been used chelatoformated sorbent on the basis of sterol-malein anhidryde sopolymer. Determination was spent by spectrophotometric method. For this purpose the reagent 2,2',3,4-tetrahydroxy-3’-sulpho-5’-chlorazobenzol (R) has been used. For creation of necessary acidity we have used phyxanal НСl (pH 0-2) and ammonium-acetate buffer solutions (pH 3-11). pH solutions were measured by ionomere I-130 with a glass electrode. Optical density of solutions measured on photocalorimetre КФК 2 (l=1cм)

Table1: Spectrophotometric characteristics of complex of uranium (VI) with R .

| pHopt | (max, nm | Composition | (мах(10-4 | Interval of submission to Beer’s law (g/ml | Constants of stability |
| --- | --- | --- | --- | --- | --- |
| 4 | 490 | 1 : 2 | 0.60( 0.02 | 0.952 – 9.520 | 5.36(0.03 |

The of sterol malein anhidryde copolymer had been modifikated with 2,4-diamin-6-phenil-triazin 1,3,5 in precense formaldegide. Sorbent synthesized by known methods [1].  The static sorbtion capacity of the received sorbent has been certain on an ion K+ (SEC=11,4 mmol/g). The sorbtion of uranium (VI) has been studied by the synthesized sorbent with influence of acidity of environment, time, and concentration of uranium (VI), ionic force on sorbtion has been investigated.

Tabl.2. Optimal conditions of concentration of uranium (VI) ions by polymer sorbent in static conditions

| SC, mg/g | pHopt | ((, mol/l | Time, clocke | d, мм |
| --- | --- | --- | --- | --- |
| 455 | 8 | 0,8 | 3,0 | 0,14 |

(- ionic force which leuds to significant reduction of sorbtion

Also the desorbtion of sorbented ions of uranium (VI) has been studied. Influence of different mineral and organic acids on desorbtion of ions has been investigated. Experiment has shown, that maximal desorbtion of uranium (VI) occurs in nitrate acid.

References

1. Aliyeva R.A., Veliyev V.N., Qamidov S.Z., Chiraqov F.M. Chemical problems. 2006. №3, 496 p.