SWITCHABLE CUCURBITURIL-BIPYRIDINE BEACONS[1]

Ofer Reany*, Mantosh K. Sinha*, Ehud Keinan*

*The Schulich Faculty of Chemistry, Technion – Israel Institute of Technology,

Haifa, Israel,

reany@tx.technion.ac.il;

Abstract text

4-aminobipyridine derivatives form strong inclusion complexes with cucurbit[6]uril, exhibiting remarkably large enhancements of fluorescence intensity and quantum yields. The remarkable complexation-induced pKa shift (ΔpKa = 3.3) highlights the strong charge-dipole interaction upon binding. The reversible binding phenomenon can be used for the design of switchable beacons that can be incorporated into cascades of binding networks.

This concept is demonstrated here by three different applications: (a) a switchable fluorescent beacon for chemical sensing of transition metals and other ligands; (b) direct measurement of binding constants between cucurbit[6]uril and various non-fluorescent guest molecules; and (c) quantitative monitoring of biocatalytic reactions and determination of their kinetic parameters. The latter application is illustrated by the penicillin G acylase-catalyzed hydrolysis of an amide and by the aldolase antibody 38C2-catalyzed elimination reaction of a β–cabamoyloxy ketone.

References

[1].	Sinha, K. M., Reany, O., Parvari, G., Karmakar, A., and Keinan, E.*; Switchable Cucurbituril-Bipyridine Beacons, Chem. Euro. J., 2009, in press.

Acknowledgements:

We are grateful to the Israel Science Foundation and the German-Israeli Project Cooperation (DIP) for their financial support. We thank the Institute of Catalysis Science and Technology, Technion, and the Skaggs Institute for Chemical Biology for the infrastructure facilities used in this study.