TAT PEPTIDE AND ITS CONJUGATES: PROTEOLYTIC STABILITY

Jacob Grunwald,3,1 Tomas Rejtar,1 Rupa Sawant,1 Zhouxi Wang,2,3 and Vladimir P. Torchilin*,1

1 - Department of Pharmaceutical Sciences and Center for Pharmaceutical Biotechnology and Nanomedicine

2 - Barnett Institute and Department of Chemistry and Chemical Biology, Northeastern University, Boston, Massachusetts 02115.

3 - While on leave from Israel Institute for Biological Research, Ness Ziona, Israel.

Grunwald7@gmail.com

The proteolytic cleavage of TATp, TATp-PEG1000-PE conjugate (TATp-conjugate), and TATp as TATp-conjugate in mixed micelles made of TATp-conjugate and PEG5000-PE (2.5% mol of TATp-conjugate, TATp-Mic) were studied by HPLC with fluorescent detection using fluorenylmethyl chloroformate (FMOC) labeling and by MALDI-TOF MS analysis. The cleavage kinetics were analyzed in human blood plasma and in trypsin-containing phosphate buffered saline (PBS), pH 7.4, to simulate the proteolytic activity of human plasma. The trypsinolysis of free TATp, TATp-conjugate, and TATp-Mic revealed that the main initial fragmentation is an endocleavage at the carboxyl terminus resulting in an Arg-Arg (RR) dimer. The trypsinolysis followed pseudo-first-order kinetics. The cleavage of the free TATp was relatively fast with a half-life of a few minutes (t1/2 ~ 3.5 min). The TATpconjugate

showed more stability with about a 3-fold increase in half-life (t1/2 ~ 10 min). TATp in TATp-Mic was highly protected against proteolysis with an over 100-fold increase in half-life (t1/2 ~430 min). The shielding of TATp by PEG moieties in the proposed TATp-Mic is of great importance for its potential use as a cell-penetrating moiety for multifunctional “smart” drug delivery systems with detachable PEG.

References

(1)  Grunwald, J. Rejtar. T. Sawant, R. Wang, Z. and Torchilin, P.T., TAT Peptide

and Its Conjugates: Proteolytic Stability. Bioconj. Chem. 20, 1531-1537, (2009).

(2) Kale, A. A., and Torchilin, V. P. Enhanced transfection of tumor cells in

vivo using “Smart” pH-sensitive TAT-modified pegylated liposomes. J. Drug

Targeting 15, 538–545, (2007).

Acknowledgment

This study was supported by the NIH grants RO1 CA121838 and RO1 CA128486 to VPT. W.C. Hartner is gratefully acknowledged for his help during this manuscript preparation.