VOLTAMMETRIC SENSING OF MERCURY AND COPPER CATIONS AT POLY(EDTA-LIKE) FILM MODIFIED ELECTRODE

George O. Buica*, Eleonora M. Ungureanu*, Christophe. Bucher**, Jean-Claude Moutet **, Guy Royal **, Eric Saint-Aman **

*Faculty of Applied  Chemistry and Material Sciences, University "Politehnica" of Bucharest, Calea Grivitei 132, 010737, Bucharest, Romania

**Université Joseph Fourier Grenoble 1, Département de Chimie Moléculaire, UMR CNRS-5250, Institut de Chimie Moléculaire de Grenoble, FR CNRS-2607, BP 53, 38041, Grenoble Cedex 9, France

em_ungureanu2000@yahoo.com

Complexing polymer-coated electrodes have been synthesized by oxidative electropolymerization of ethylenediamine tetra-N-(3-pyrrole-1-yl)propylacetamide (monomer L) [1].

Structural formula of L

The presence of four polymerizable pyrrole fragments on the same EDTA skeleton was thought to confer enhanced rigidity and controlled dimensionality to the resulting complexing materials, which were used for the electrochemical detection of Hg(II), Cu(II), Pb(II) and Cd(II) ions by means of the chemical preconcentration-anodic stripping technique. The polyamide electrode material showed particularly a significant selectivity towards mercury ions, even in the presence of a large excess of other metal cations. Moreover, the use of imprinted polymer-coated electrodes prepared by electropolymerization of L in the presence of metal cations turned out to significantly improve the detection limits, down to 5 × 10–10 mol L–1 for Hg(II) and Cu(II) species.

References

G.-O. Buica, C. Bucher, J.-C. Moutet, G. Royal, E. Saint-Aman, E. M. Ungureanu, Electroanalysis, 2009, 21(1), 77-86.

Acknowledgements: The financial support of this research, received from CNMP 71-067 REMORESE project, is gratefully acknowledged.